Author: Carlos Germosen Polanco

Advisor: Rufina G. Alamo

Title: Properties of Crystalline Polyethylene-Like Materials Under Industrially Relevant Processing Conditions

Location: FAMU-FSU College of Engineering, Department of Chemical and Biomedical Engineering, 2525 Pottsdamer St, Tallahassee, FL, 32310. USA

Building and room number: CE2 B202B

Date: 11/9/2021

Start time: 04:00 PM

End Time: 06:00 PM

Email: cg19n@my.fsu.edu

Abstract

Polyethylene-like materials with in-chain acetal units (-O-CH2-O-) precisely spaced by long methylene runs (between 12 and 26 CH2), crystallize from the melt in four different crystallographic forms (polymorphs) depending on the depth of undercooling. The polymorphs were characterized via wide angle X-ray diffraction as disordered, hexagonal, Form I, and Form II phases with increasing crystallization temperature. Classical differential scanning calorimetry (DSC) demonstrated that the transition from Form I to Form II occurs in a narrow temperature range (< 1°C). At the transition, there is a minimum in the crystallization rate and extremely low levels of crystallinity. The latter recovers at temperatures above the transition. Because the disordered and hexagonal phases of these long-spaced polyacetals develop at large undercooling, not accessible by DSC, in the present work we have used fast scanning calorimetry (FSC) to obtain isothermal crystallization rates and heats of fusion of these samples. All polyacetals display inversions in the crystallization rate and low heat of fusion at the transition temperature between the disordered and hexagonal form, as well as in the transition between hexagonal and Form I polymorphs. These results, which indicate a general behavior of precision polyethylene-like materials reveal critical structure-property relationships needed for tuning industrial melt processing conditions of these and similar sustainable polymers.